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1. SCOPE & PURPOSE
The content of this report will evaluate based on the major and minor defects and what they could mean, appropriate recommendations on maintenance and remedial measures, technical information on the construction/topography of the property/land, building materials integrity, and requirements for any further specialist investigation.

This report should not be considered as a full detailed structural analysis report, but as a reasonable attempt based on observations and determinations of defects focused on the structural elements of the building and gave opinions as to whether the components are performing intentionally or in need of immediate repair. Other necessary recommendations incorporated are for the structure to be adequate, cost effective and safe. 

2. CONVENTIONS USED IN THIS REPORT 
	Convention
	Codes
	Description

	SATISFACTORY
	S
	Indicates the component is functionally consistent with its original purpose but 
may show signs of normal wear and tear and deterioration.

	MARGINAL
	M
	Indicates the component will probably require repair or replacement anytime within five 
years.

	POOR
	P
	Indicates the component will need repair or replacement now or in the very near future.

	MAJOR CONCERNS
	MC
	A system or component that is considered significantly deficient or is unsafe.

	SAFETY HAZARD
	SH
	Denotes a condition that is unsafe and in need of prompt attention.

	NOT APPLICABLE 
	NA
	This Component is not considered to be part of the building or within the scope of survey.



3. AERIAL SITE MAP
[image: ]
Figure 1. Tourism Office Site Location.

	4. SITE SURVEY DATA CHECKLIST.

	A
	SURVEY DESCRIPTION

	TYPE OF SURVEY
	Structural Appraisal 

	REPORT NO.
	001
	DATE
	07/10/26

	ADDRESS
	Betio, Tarawa
	WEATHER
	Sunny

	PREPARED BY
	Maria Betaia, Tekaewaka Mwaio

	PREPARED FOR
	MTCIC

	COORDINATES
	1°21'32.06"N 172°56'01.83"E

	ATTENDEES
	MTCIC OM, Maria, Tekaewaka

	OWNERSHIP
	☒ Government owned  ☐ NGO-owned  ☐ Private-owned


	A1  
	STRUCTURAL APPRAISAL

	[bookmark: _Hlk193116577]Descriptions
	Checked (x)
	convention
	Comments

	
	Yes
	No
	
	

	1. BUILDING DETAILS

	1.1. As-built Details

	1.1.1. [bookmark: _Hlk193119305]Building Classification
	☐ Class 1[footnoteRef:1]      ☐  Class 2[footnoteRef:2]       ☒  Class 3[footnoteRef:3]    ☐ Others[footnoteRef:4]    [1:  Building class 1 refers to a residential building ]  [2:  Building class 2 refers to a residential building occupied by a number of unrelated persons, e.g. boarding-house, dormitory, accommodation for aged, disabled or children, etc]  [3:  Building class 3 refers to all other buildings including office buildings, shops, warehouse, assembly house, etc 
4 Other building works indicated under Schedule 1 of the Building Act 2006]  [4: 
] 


	1.1.2. Building Type
	☒ Office  ☐ Classroom  ☐ Warehouse ☐ Mwaneaba/Hall
☐ Ablution Block ☐ Residential 
☐ Others _______________________________


	1.1.3. Occupancy
	Not Occupied

	1.1.4. Usage
	Office

	1.1.5. Building/Room Name
	Kiribati Visitors Information Center

	1.1.6. Approx Age of building
	n/a

	1.1.7. Main entrance face
	South 

	1.1.8. No. of Buildings
	1

	1.1.9. No. of Floor Levels
	2

	1.2. Survey Scope

	1.2.1. Ground level
	x
	
	3 office rooms and 1 washroom.

	1.2.2. 1st floor level
	x
	
	3 office rooms

	1.2.3. Roofing level
	x
	
	

	2. MAIN BUILDING ELEMENTS CHECKED

	2.1. Walls
	
	
	
	

	2.1.1. External walls
	x
	
	P
	☒Concrete/brick  ☒Timber  ☐others 
1st floor concrete wall showing hairline cracks on the North and east side of the building. Under the windowsills, bond beam and corner end of the building. To be repaired 1st floor level external lining to be repaired and matched with existing material. 

	2.1.2. Internal Walls
	x
	
	P
	☒Concrete/brick   ☒Timber  ☐others
Timber partition wall required repair for the common office room at the ground floor. Toilet concrete wall shows hairline cracks to be repaired. 

	2.1.3. Door(s)
	x
	
	P
	Shared office door to be repaired at the ground floor. 

	2.1.4. Window(s)
	x
	
	P
	All broken louvers are to be replaced with the building’s window.

	2.1.5. Opening frames
	x
	
	P
	Door framing for the common office at ground floor to be fixed with the partition timber wall.

	2.2. Roof
	
	
	
	

	2.2.1. Type 
	
	
	
	☒Pitch roof  ☐Half truss ☐Flattop ☐others

	2.2.2. Ceiling
	x
	
	MC
	Ground floor ceiling requires repair, change ceiling nails to screws. 

	2.2.3. Gable end(s)
	x
	
	P
	Require replacement for lining for cable ends on the west end of the roof.

	2.3. Electrical installation
	
	
	
	

	2.3.1. Wiring
	x
	
	MC
	Needs re-wiring arrangement for power ports that have detached from ceilings.

	2.3.2. Main switch board
	
	
	
	

	2.3.3. Power ports
	x
	
	MC
	To be checked for rack re-attachment. 

	2.3.4. Lights
	x
	
	MC
	Light bulbs to be changed and light units to be re-fixed to ceiling for ground level and 1st level lightings. 

	2.3.5. Air conditioning
	x
	
	MC
	All indoor AC unit racks need to be checked and re-installed. 

	3. OTHER BUILDING COMPONENTS 

	3.1. Walkway/Ramp/Stairs 
	
	
	
	

	3.1.1. Accessibility
	x
	
	P
	The stairways require replacement for wall lining. 

	3.2. Balcony/Terrance 
	
	
	
	

	3.2.1. Floor type
	x
	
	P
	Timber framing, West end of the balcony requires repair for floor beam replacement and landing.







	[bookmark: _Hlk192762045]B
	INSPECTION PHOTOS

	Images
	Comments

	[image: ]
	West side of the building with broken window louvers, and gable end lining. 

To be removed and replaced. 

Materials 
Window – clear glass louvers
Gable end lining – fiber cement sheet

	[image: ]
	Corner of the east to north wall behind the gutter down pipe. Crack repairing is required. 

Material – cement mortar mix.
Repair method is up to the contractor’s recommendation in relation to the material provided. 

	[image: ][image: ]
	Hairline crack on the internal wall for office corridor and toilet. Requires repair. 

Material – cement mortar
Repair methods are up to the contractor’s recommendation in relation to the material provided.

	
	

	[image: ][image: ][image: ]
	The 1st floor external linings require replacement of broken cement fiber sheets around the 1st floor. The figure provided of the wall needs changing for the external and internal wall lining.

External wall – fiber cement sheet
Internal wall – Masonite sheet



	[image: ]
	Stairways wall lining to remove damaged walls and replace.

Material – fiber cement sheet.

	[image: ][image: ][image: ]
	Common office door, to be repaired with the wall partition and door framing.

Registry counter to be repaired for the corner towards the common rooms door. 

	[image: ][image: ]
	Ceiling to be repaired and lighting units to be fixed to the ceiling. Bulbs for all lights are to be checked for replacement.

AC units and power points to be re-racked onto wall. 



	[image: ]
	The bond beams behind the AC unit to be repaired as recommended for the repair method of the concrete cracks.





5. ENGINEERING REPORT & RECOMMENDATIONS 
All recommendations are to be applied which are mentioned beside the attached figures. 

6. CONCLUSION REMARKS 
The survey data concludes that the overall condition of the building is structurally safe but with an overall Poor convention, which requires all recommendations to be repaired for the building to be useable and to be occupied.

Therefore, MISE -QCID strongly recommended that the repairs be undertaken immediately to stabiles the building condition. However, the above recommendations need to be completed as to expand its structural elements performance and lifetime of the building. 
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